### Primary Batteries

Leclanché Cells(zinc carbon or dry cell)

Anode: Zinc

Cathode: Manganese Dioxide (MnO2)

Electrolyte: Ammonium chloride or zinc chloride dissolved in water

Applications: Flashlights, toys, moderate drain use

The basic design of the Leclanché cell has been around since the 1860s, and until World War II, was the only one in wide use. It is still the most commonly used of all primary battery designs because of its low cost, availability, and applicability in various situations. However, because the Leclanché cell must be discharged intermittently for best capacity, much of battery research in the last three decades has focused on zinc-chloride cell systems, which have been found to perform better than the Leclanché under heavier drain.

This figure shows typical discharge curves for general-purpose Leclanché zinc chloride D-size cells discharge 2 h/day at 20º C. Solid line—zinc chloride; broken line—Leclanché (Linden 8.18). The zinc-chloride cell has a higher service life and voltage than the Leclanché (at both higher and lower discharge rates).

In an ordinary Leclanché cell the electrolyte consists (in percent of atomic weight) of 26% NH4Cl (ammonium chloride), 8.8% ZnCl2 (zinc chloride), and 65.2% water. The overall cell reaction can be expressed:

Zn + 2MnO2 +2NH4Cl —> 2MnOOH + Zn(NH3)2Cl2 E=1.26

The electrolyte in a typical zinc chloride cell consists of 15-40% ZnCl2 and 60-85% water, sometimes with a small amount of NH4Cl for optimal performance. The overall cell reaction of the zinc chloride as the electrolyte can be expressed:

Zn + 2MnO2 + 2H2O + ZnCl2 —> 2MnOOH + 2Zn(OH)Cl

MnO2, is only slightly conductive, so graphite is added to improve conductivity. The cell voltage increases by using synthetically produced manganese dioxide instead of that found naturally (called pyrolusite). This does drive the cost up a bit, but it is still inexpensive and environmentally friendly, making it a popular cathode.

These cells are the cheapest ones in wide use, but they also have the lowest energy density and perform poorly under high-current applications. Still, the zinc carbon design is reliable and more than adequate for many everyday applications.

- Alkaline Cells

Anode: Zinc powder

Cathode: Manganese dioxide (MnO2) powder

Electrolyte: Potassium hydroxide (KOH)

Applications: Radios, toys, photo-flash applications, watches, high-drain applications

This cell design gets its name from its use of alkaline aqueous solutions as electrolytes. Alkaline battery chemistry was first introduced in the early ’60s. The alkaline cell has grown in popularity, becoming the zinc-carbon cell's greatest competitor. Alkaline cells have many acknowledged advantages over zinc-carbon, including a higher energy density, longer shelf life, superior leakage resistance, better performance in both continuous and intermittent duty cycles, and lower internal resistance, which allows it to operate at high discharge rates over a wider temperature range.

Zinc in a powdered form increases the surface area of the anode, allowing more particle interaction. This lowers the internal resistance and increases the power density. The cathode, MnO2, is synthetically produced because of its superiority to naturally occurring MnO2. This increases the energy density. Just as in the zinc carbon cell, graphite is added to the cathode to increase conductivity. The electrolyte, KOH, allows high ionic conductivity. Zinc oxide is often added to slow down corrosion of the zinc anode. A cellulose derivative is thrown in as well as a gelling agent. These materials make the alkaline cell more expensive than the zinc-carbon, but its improved performance makes it more cost effective, especially in high drain situations where the alkaline cell's energy density is much higher.

The half-reactions are:

Zn + 2 OH- —> Zn(OH)2 + 2 e-  (also written as Zn + 2 OH- —> ZnO + H2O + 2 e-)

2 MnO2 + H2O + 2 e- —>Mn2O3 + 2 OH-

The overall reaction is:

Zn + 2MnO2 —> ZnO + Mn2O3 E=1.5 V

There are other cell designs that fit into the alkaline cell category, including the mercury oxide, silver oxide, and zinc air cells. Mercury and silver give even higher energy densities, but cost a lot more and are being phased out through government regulations because of their high toxicity as heavy metals. The mercury oxide, silver oxide, and zinc air (which is being developed for electronic vehicles) are all discussed below.

Source: http://www.powerstream.com/BatteryFAQ.html?nowritefs